CSI - SECTION 09 83 16

Acoustic Plaster - AP335 - 48mm system - Type A mount

PART 1 GENERAL

1.1.	SECTION INCLUDES

All bonding of pre-base coated mineral wool boards as well as on-site application of seamless acoustical plaster finish. Extent of work to be shown on drawings.

1.2.	RELATED SECTIONS

- Section 05 40 00 – Cold-Formed Metal Framing

- Section 06 20 00 – Finish Carpentry

- Section 09 29 00 - Gypsum Board

1.3.	REFERENCES

- ASTM C423 - Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

- ASTM E 84 - Standard Test method for Surface Burning Characteristics of Building Materials.

- ASTM D 3273 – Standard Test Method for Resistance to the Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber.

- CDPH Standard Practice for VOC Testing – Method v1.2.

- ISO 11890-2 – Paints and varnishes – Determination of Volatile organic compounds (VOC) and/or semi volatile organic compounds (SVOC) content – Part 2: Gas-chromatographic method.

1.4.	SYSTEM PERFORMANCE REQUIREMENTS

Armourcoat Acoustic Plaster – AP335 shall be tested by a qualified independent testing agency for the following properties according to the following test methods:

- Noise Reduction Coefficient: NRC 0.90 (SAA 0.92) – ASTM C423 – Direct Mount (Type A).

Flame Spread: Class A (FSI = 15 : SDI = 10) - ASTM E84.

Mold Growth: 10, No Defacement - ASTM D3273.

VOC Emissions – Between 0.5 and 5.0 mg/m3, Passes requirement for classroom and office use – CDPH Method v1.2.

VOC Content – Acoustic Topcoat AP335 = <1.0 grams / liter – ISO 11890-2

1.5.	SUBMITTALS

See Section 01300 - Administrative Requirements, for submittal procedures.

- Product Data: Provide manufacturer’s technical data on products specified, including installation instructions.

- LEED Submittals: Provide all details pertaining to system and LEED data per Armourcoat document:

AI-40-109ST21.01.01: LEED STATEMENT – ARMOURCOAT ACOUSTIC PLASTER – 48mm SYSTEM.

- Shop Drawings: Indicate designs, colors, and locations.

- Samples: Submit [_____] samples, 6 x 6 inches in size, illustrating finish color and texture.

- Qualification Data: Certificate issued by distributor indicating that installer has attended training class and is authorized to install specified product.

- Warranty: Sample copy of manufacturer's Five-Year Limited Materials Warranty stating obligations, remedies, limitations, and exclusions of warranty.

1.6.	QUALITY ASSURANCE

- Installer Qualifications: Company specializing in performing work of this Section with a minimum of one-year documented experience. Include list of at least three completed projects of similar scope with project names and addresses and names and addresses of architects and owners. Installers must have attended Armourcoat training class.

- Single Source Responsibility: Provide only proprietary, factory-formulated materials as produced by Armourcoat, Ltd. specifically for applications indicated. Substitutes within the system are not permitted.

- Fire-Test-Response Characteristics: Provide finished system with the following surface-burning characteristics as determined per ASTM E 84 by UL or another testing and inspecting agency acceptable to authorities having jurisdiction.

- 1.	Flame Spread: 15 or less.
2.	Smoke Contribution: 10 or less.

1.7.	MOCK-UP

- Prior to installing Acoustic plaster, construct mock-up of finished surface, [______] feet long by [______] feet wide, illustrating surface [design,] finish and color.

- Locate where [directed by Architect / indicated on drawings].

- Mock-up [may / may not] remain as part of the Work.

1.8.	DELIVERY, STORAGE AND HANDLING

- Deliver materials to the construction site in their original packaging with manufacturer’s labels identifying manufacturer and product; color designation; lot number; and date of manufacture.

Inspect materials upon delivery and immediately report to Architect damaged or defective materials.

Store materials in an interior well ventilated area with minimum ambient temperature of 54º F 
(12º C). Prevent deterioration due to moisture, temperature changes, contamination, or other causes.

1.9.	PROJECT CONDITIONS

- Environmental Requirements: Do not apply Acoustic plaster materials when substrate or ambient air temperatures is under 54º F (12º C) or over 95º F (35ºC).

- Maintain these conditions 24 hours before, during and after installation of Acoustic plaster system.

1.10.	WARRANTY

- See Section 01780 - Closeout Submittals, for additional warranty requirements.

- Provide manufacturer’s standard written warranty.

- 1.	Period of Warranty: 5 years.

PART 2 PRODUCTS

2.1.	MANUFACTURERS

- Acceptable Manufacturers:

- 1.	Armourcoat Surface Finishes, Inc., 4330 Production Court, Las Vegas, Nevada 89115, USA 	Tel: 702 644 0606. Fax: 702 644 0554. E-mail: sales@usa.armourcoat.com.

- 2.	Armourcoat Ltd., Morewood Close, London Road, Sevenoaks Kent. TH13 2HU.  
	Tel: +44 (0) 1732 460668. Fax: +44 (0) 1732 450930. 						E-mail: sales@armourcoat.co.uk  Web: www.armourcoat.com.

- Substitutions: Not permitted.

2.2.	PRODUCTS

- Products: Armourcoat Acoustic Plaster materials, Armourcoat Ltd.

- Design:[Custom design as shown on architectural drawings and as approved on shop drawings]

- Finish: [Custom finish to match Architect’s approved sample]

- Color: [_____________) / Multiple colors as indicated on Schedule at end of this Section].

2.3.	MATERIALS

- Acoustic Plaster System: Provide manufacturer’s complete system of proprietary materials specifically formulated for compatibility with one another including:

- 1.	Armourcoat Bondplast
	40mm Mineral Wool Boards (pre coated with Armourcoat Acoustic Board Coating)
	Armourcoat Acoustic Undercoat Granules
	Armourcoat Acoustic Undercoat Resin
	Armourcoat Acoustic Topcoat – AP335
	Colorant [if required]

- Water: Clean, fresh, potable, and free of mineral or organic matter which can affect plaster.

PART 3 EXECUTION

3.1.	EXAMINATION

- Verify the suitability of existing conditions before starting work. Do not begin Work of this Section until unsatisfactory conditions have been corrected.

Verify Gypsum substrates are true and level and finished to a Level 1 finish. Substrates and all fixtures should be sealed airtight to avoid any passage of air between the room and the plenum.

3.2.	PREPARATION

- Comply with manufacturer's written instructions for substrate preparation. Apply Acoustic Plaster to Regular Gypsum Board that complies with ASTM C 1396.

- Remove hardware, electrical switch and outlet plates, lighting fixtures and other items already in place that are not to receive plaster finish.

- 1.	After completion of work, reinstall items using workers skilled in the trades involved.

- Protect adjacent surfaces and items that are not to receive plaster finish, but which cannot be removed, from finish work. Use masking materials that will not damage protected items and surfaces.

- Clean substrates of substances that could impair bond including mold, mildew, oil, grease, salts, contamination, and dirt using methods recommended by manufacturer.

- Prepare all materials in accordance with manufacturer’s recommendations.

3.3.	INSTALLATION

- Prepare perimeter wall with beads or wax tape to avoid Acoustic system bonding to any wall sections.

- Around any light fittings or openings install adhesive backed air-tight tape.

- Prepare and fix all required pattresses. Bond all Acoustic Base panels using Armourcoat Bondplast.

- Check the alignment between panels and sand out any lipping or discrepancies.

- Mix and apply the acoustic undercoat to the entire surface, filling up to the edge beads and over the panel joints.

- Check the surface flatness and lightly sand where necessary.

- Apply Acoustic Topcoat Plaster in accordance with manufacturer’s instructions.

- Provide finish free of unsightly variations in texture and other defects.

3.4.	CLEANING AND PROTECTION

- Remove temporary coverings used to protect adjacent surfaces and reinstall hardware, plates, lighting fixtures and other items previously removed.

- Clean and repair adjacent surfaces and items soiled or damaged during Work of this Section.

- Maintain and protect completed Acoustic plaster surfaces until time of acceptance at Substantial Completion.

3.5.	SCHEDULE

- Plaster Style A:

- 1.	Location: [______/ As indicated on drawings].
2.	Design: [______].
3.	Finish: [______].
4.	Color: [______].

Plaster Style B:

- 1.	Location: [______/ As indicated on drawings].
2.	Design: [_____].
3.	Finish: [_____].
4.	Color: [_____].